BioSLIP® 275

Hard Bio-Based wax alloy

Shamrock’s product line of micronized waxes is primarily designed to provide rub and abrasion resistance.

# Product Description:

BioSLIP® 275 is a biobased hard wax alloy that has components showing melting peaks ranging from 125 – 128°C.

# Application:

BioSLIP® 275 is used in both air dry and baked coatings for solvent and aqueous systems at 1-3% of total formula weight.

# Features and Benefits:

Typical Properties:

Abrasion Resistance Mar/Scuff

Appearance:	White Wax Powder

Specific Gravity:	0.98

Particle Size Mean Value:	5 µm

99% of Particle Under:	22 µm

- Hegman Grind:	7.0 Min

# Regulatory Status:

The components of this product are listed on multiple chemical inventories. For specific information on the applicable chemical inventories, please refer to the product SDS.

# Safety, Shipping and Handling:

For complete safety, shipping and handling information please contact your regional Customer Service Representative, or our Customer Service Team at customerserviceteam@shamrocktechnologies.com.

For more information about Shamrock’s other products or capabilities please visit us at our website, ShamrockTechnologies.com.